JASxIBC P-1000 50Ah Mid-Ni Process Doc (Rev 7)

Contents:  Revision Log   ·   Material Spec   ·   Anode Mix   ·   Anode PressSlit   ·   Cathode Mix   ·   Cathode CoatDry   ·   Cathode PressSlit   ·   Assembly   ·   Finishing   ·   Formation   ·   ElectrodeAssembly OCAP

# Revision Log

| Revision | Comments | Editors | Date |
| --- | --- | --- | --- |
| 7.0 | Revised based on SH plant visit 4/14-24 '26 Process parameters were revised. Updated Formation Recipe to Fast Formation. Added OCAP. Added Travelers tabs. Added notes on maintenance for each electrode processing step. | Nayon, Bruce, Kunal | 2026-05-07 |

## June 2026 Graphite Trials

| QCG X9L | Umicore 622 | validate | lowest cost |
| --- | --- | --- | --- |
| QCG X9L | POSCO 622 | validate |  |
| Himadri | Umicore 622 |  |  |
| QCG X9 | POSCO 622 |  |  |

# Material Spec

Incoming quality control (IQC) specifications for all purchased raw materials, listing each supplier's CoA target alongside the measured sample value.

## Raw Materials for Anode

| Category | Product | Supplier CoA | Material Property |  | Material Spec | Sample (listed in CoA) |
| --- | --- | --- | --- | --- | --- | --- |
| AAM | Graphite QCG-X9 | ShanShan | D10 (µm) |  | 7.7 ±1.5 | 9.0 |
|  |  |  | D50 (µm) |  | 14.0 ±1.5 | 14.7 |
|  |  |  | D90 (µm) |  | 24.6 ±2.0 | 23.3 |
|  |  |  | Tap Density (g/cm3) |  | 1.00 ±0.05 | 0.99 |
|  |  |  | BET (m2/g) |  | 1.0 ±0.5 | 1.1 |
|  |  |  | Fe (ppm) |  | <50 | not provided |
|  |  |  | Magnetic Impurity (ppb) |  | <100 | 70 |
|  |  |  | Moisture (ppm) |  | <500 | not provided |
|  |  |  | Discharge Capacity at 0.1C, LL ~10 (mAh/g) |  | >347 | 352.7 |
|  |  |  | 1st CE % |  | >92.3% | 92.7 |
| Carbon Additive | Super-P | Imerys | Carbon Content (%) |  | >99.5 | >99.5 |
|  |  |  | Settle Density (kg/m3) |  | 160 ±20 | 160 |
|  |  |  | BET (m2/g) |  | 62.0 ±5.0 | 61.3 |
|  |  |  | Moisture (%) |  | <0.3 | 0.1 |
|  |  |  | pH |  | 8.0-11.0 | 9.7 |
|  |  |  | Sulfur Content (%) |  | <0.030 | 0.021 |
|  |  |  | Volatiles Content (%) |  | <0.15 | 0.10 |
|  |  |  | Ash Content (%) |  | <0.025 | 0.010 |
|  |  |  | Trace Metal Content (ppm) |  | <5.0 | <3.0 |
|  |  |  | Toluene Extract (%) |  | <0.10 | <0.10 |
| Binder - CMC | powder | GL Chem | Viscosity (cP) of 1.0 wt% soln |  | 2,000-3,000 | 2,320 |
|  |  |  | pH |  | 6.7-7.7 | 7.35 |
|  |  |  | Deg of Substitution |  | 0.8-1.0 | 0.9 |
|  |  |  | Number of Micro-gel (ea/25cm2) |  | <30 | 20 |
|  |  |  | NaCl (%) |  | <0.3 | 0.06 |
| Binder - SBR | 40 wt% solution | Hansol Chem | Solid Content (wt%) |  | 40.0 ±0.5 | 40.2 |
|  |  |  | pH |  | 2026-07-09 | 8.1 |
|  |  |  | Particle Size (nm) |  | 120-220 | 162.5 |
|  |  |  | Viscosity (cP) |  | <100 | 16.5 |
| Solvent | DI water | Sourced onsite | Resistivity (MOhm.cm) |  | >15 | 18.2 |

## Raw Materials for Cathode

| Category | Product | Supplier CoA | Material Property |  | Material Spec | Sample (listed in CoA) |
| --- | --- | --- | --- | --- | --- | --- |
| CAM | NMC-622 | Umicore | D10 (µm) |  | 6.0 ±1.0 | 6.1 |
|  |  |  | D50 (µm) |  | 11.5 ±1.0 | 11.3 |
|  |  |  | D90 (µm) |  | 20.0 ±2.0 | 19.9 |
|  |  |  | Moisture (%) |  | <0.020 | 0.014 |
|  |  |  | Tap Density (g/cm3) |  | 2.6 ±0.2 | 2.6 |
|  |  |  | BET (m2/g) |  | 0.3 ±0.1 | 0.29 |
|  |  |  | Ni mol% |  | 60.0 ±0.2 | 60.1 |
|  |  |  | Mn mol% |  | 20.0 ±0.2 | 19.9 |
|  |  |  | Co mol% |  | 20.0 ±0.2 | 19.9 |
|  |  |  | Ca wt% |  | <0.010 | 0.006 |
|  |  |  | Cu wt% |  | <0.010 | 0.000 |
|  |  |  | Fe wt% |  | <0.010 | 0.000 |
|  |  |  | Na wt% |  | <0.050 | 0.031 |
|  |  |  | Discharge Capacity at 0.1C, LL ~20 (mAh/g) |  | >175 | not provided |
|  |  |  | 1st CE % |  | >89% | not provided |
| Carbon Additive | Super-P | Imerys | Carbon Content (%) |  | >99.5 | >99.5 |
|  |  |  | Settle Density (kg/m3) |  | 160 ±20 | 160 |
|  |  |  | BET (m2/g) |  | 62.0 ±5.0 | 61.3 |
|  |  |  | Moisture (%) |  | <0.3 | 0.1 |
|  |  |  | pH |  | 8.0-11.0 | 9.7 |
|  |  |  | Sulfur Content (%) |  | <0.030 | 0.021 |
|  |  |  | Volatiles Content (%) |  | <0.15 | 0.10 |
|  |  |  | Ash Content (%) |  | <0.025 | 0.010 |
|  |  |  | Trace Metal Content (ppm) |  | <5.0 | <3.0 |
|  |  |  | Toluene Extract (%) |  | <0.10 | <0.10 |
| Binder 1 - PVDF | Solef 5130 | Solvay | Intrinsic Viscosity (l/g) |  | 0.270-0.310 | 0.286 |
|  |  |  | Volatiles Content (%) |  | <0.20 | 0.06 |
|  |  |  | Melting Point (°C) |  | 160.0-168.0 | 163.3 |
| Binder 2 - PVDF | Solef 6020 | Solvay | MFI @ 230°C / 21.6 kg (g/10min) |  | 0.7-2.0 | 1.0 |
|  |  |  | Volatiles Content (%) |  | <0.20 | 0.04 |
|  |  |  | Melting Point (°C) |  | >170.0 | 170.3 |
|  |  |  | Median Particle Size D50 (µm) |  | 70-140 | 114 |
| Solvent | NMP | Jaewon | Purity wt% |  | >99.8 | 99.94 |
|  |  |  | Moisture (ppm) |  | <300 | 82 |
|  |  |  | Color on APHA |  | <20 | 3 |
|  |  |  | Trace Metal (ppb) |  | <20 | <0.2 |

## Raw Materials for Electrode, Cell Assembly, and Shipping

| Cathode Foil | Al foil | Dongil | TBD |  | TBD |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | TBD |  | TBD |  |  |
|  |  |  | TBD |  | TBD |  |  |
|  |  |  | TBD |  | TBD |  |  |
|  |  |  | TBD |  | TBD |  |  |
|  |  |  | TBD |  | TBD |  |  |
|  |  |  | TBD |  | TBD |  |  |
| Anode Foil | Cu foil | SK Nexilis | TBD |  | TBD |  |  |
| Electrolyte | LiPF6 1.3M in EC/EMC=27/75 (v/v) + VC 2%, FEC 1%, PS 1% | Dongwha | EC wt% |  | 24.40 ±1.00 | 24.41 |  |
|  |  |  | EMC wt% |  | 56.12 ±1.00 | 56.08 |  |
|  |  |  | LiPF6 wt% |  | 15.64 ±0.50 | 15.43 |  |
|  |  |  | VC wt% |  | 1.73-2.11 | 1.95 |  |
|  |  |  | FEC wt% |  | 0.96 ±0.10 | 0.97 |  |
|  |  |  | PS wt% |  | 0.96 ±0.10 | 0.95 |  |
|  |  |  | Moisture (ppm) |  | <20 | 5.55 |  |
|  |  |  | HF (ppm) |  | <80 | 15.28 |  |
|  |  |  | SO4 (ppm) |  | <10 | 0.120 |  |
|  |  |  | Trace Na, Cl, K, Ca, Fe, Pb (ppm) |  | <5 | <0.3 |  |
|  |  |  | Color on APHA |  | <100 | 6 |  |
|  |  |  | Density at 25°C (g/cm3) |  | not provided | 1.228 |  |
| Separator | Double ceramic (2+2 µm) coated PE (9 µm) | Horizon | Width (mm) |  | 126.0 (+0.5) | 126.1 |  |
|  |  |  | Thickness (µm) |  | 13.0 ±2.0 | 13.52 |  |
|  |  |  | Permeability (s/100mL) |  | 170 ±50 | 172 |  |
|  |  |  | Surface Density (g/m2) |  | 10.9 ±3.0 | 10.8 |  |
|  |  |  | Porosity (%) |  | 40 ±5 | 41 |  |
|  |  |  | Puncture Strength (gf) |  | >400 | 663 |  |
|  |  |  | Thermal Shrinkage MD (kgf/cm2) |  | <3.5 | 1.07 | *120°C/1h |
|  |  |  | Thermal Shrinkage TD (kgf/cm2) |  | <3.0 | 0.45 | *120°C/1h |
|  |  |  | Tensile Strength MD (kgf/cm2) |  | >1,400 | 2,126.20 |  |
|  |  |  | Tensile Strength TD (kgf/cm2) |  | >1,300 | 1,653 |  |
|  |  |  | Water Content (ppm) |  | <1000 | 696 |  |
| Tape |  | Daehyun ST |  |  |  |  |  |
| Can/Cap/Terminal |  |  | dimensions |  |  |  |  |
|  |  |  | short test |  |  |  |  |
| Packaging | Pad, tray | VF Package |  |  |  |  |  |
|  | Paper | Daekyung |  |  |  |  |  |

# Anode Mix

## Pre-set Conditions

| Room Dew Point (°C) | <-20 |
| --- | --- |
| Room Temperature (°C) | 23 |
| Chiller Temperature (°C) | 13 |

## Raw Materials

| Category | Product |  | Phase | Input mass (kg) | Dry mass (kg) | Solid comp (%) | Supplier Note |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AAM | Graphite |  | powder | 40.000 | 40.00 | 96.0% | ShanShan |
| Binder 1 | CMC powder |  | solid | 0.500 | 0.50 | 1.2% | GL Chem |
| Binder 2 | SBR solution |  | 40 wt% soln | 1.875 | 0.75 | 1.8% | Hansol Chem |
| Additive 1 | Super-P |  | solid | 0.420 | 0.42 | 1.0% | Imerys/C-nergy |
| Solvent | DI water |  | liquid | 40.500 | N/A | N/A |  |

Batch totals: Solid content 50.0%, Total mass 83.30 kg, Total volume 59.5 L.

## Slurry Quality Metrics

| Measurement |  | Target value | Range |
| --- | --- | --- | --- |
| Slurry Viscosity (cP) S65, 5 rpm |  | 7,000 | ± 500 |
| Slurry Viscosity (cP) S65, 50 rpm |  | 6,500 | ± 500 |
| Slurry Particle Size (µm) |  | <30 | store image |
| Slurry Density at 23°C (g/cm3) |  | 1.40 |  |
| Slurry Solid Content (wt%) |  | 50 | ± 2 |

## Additional Notes on Anode Mixing

Viscosity is the primary metric to achieve within target value.

When adding powder, ramp up agitation speed from the lowest setting (5/100 rpm) and increase in 2 to 5 or 100 rpm increments until all loose powder is incorporated. Start with Dispersion blade. Scrape the agitation blades after every powder addition step (i.e. graphite, Super-P).

Pay close attention to the slurry temperature - very important for meeting the viscosity target consistently.

Make sure the chiller is always connected to the main tank and running.

Viscosity can increase after degassing step.

For other troubleshooting, refer to the "OCAP" tab.

## Anode Recipe Steps - Single Vessel Mix

| Equipment | Step | Process |  | Amount (kg) | Solid Content (%) | RPM |  | Time (min) | Target Slurry Temp (°C) | Target Viscosity (cP) | Vessel Pressure | Note |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Planetary | Dispersion |  |  |  |  |  |
| Main Mixer (100 L) | 1 | Add CMC powder |  | 0.500 | 100.0% | 20 | 1500 | 2-4 hours until dissolved | 20-23 |  | atm | Scrape the mixer wall & bottom every 30-60 min until dissolved |
|  | 2 | Add DI water |  | 37.960 | 1.3% |  |  |  |  |  |  |  |
|  | 3 | Lower RPM to degas and measure binder viscosity |  |  |  | 5 | 900 | 60 |  | 5,000-6,000 | -0.08 MPa | Stablized binder can be used up to 1-2 weeks |
|  | 4 | Lower RPM to continue degassing and binder stabilization |  |  |  | 5 | 0-300 | 60 |  |  | atm |  |
|  | 5 | Add Super-P |  | 0.420 | 2.4% | 20 | 1700 | 30 |  |  | atm |  |
|  | 6 | Scrape the blades and continue mixing |  |  |  | 20 | 1700 | 90 |  |  | atm |  |
|  | 7 | Add Graphite |  | 40.000 | 51.9% | 20 | 1700 | 30 |  |  | atm | Expect temp rise to 25-26°C |
|  | 8 | Scrape the blades and continue mixing |  |  |  | 20 | 1700 | 90 |  |  | atm |  |
|  | 9 | Add SBR solution |  | 1.875 | 51.6% | 20 | 1700 | 120 |  | 9,000-11,000 | atm |  |
|  | 10 | Add DI water |  | 2.50 | 50.1% | 20 | 1700 | 30 |  | 6,500-8,000 | atm |  |
|  | 11 | Add DI water (calculated) |  | 0.50 | 49.8% | 20 | 1700 | 30 |  | 5,700-6,700 | atm |  |
|  | 12 | Add DI water (as needed) |  | 0.00 | 49.8% | 20 | 1700 | 30 |  |  | atm |  |
|  | 13 | Stabilize the slurry (overnight if needed) |  |  |  | 5 | 0 | 30 |  |  | atm |  |
|  | 14 | Measure viscosity and solid content (before coating) |  |  |  |  |  |  |  | 6,500 ±500 |  |  |

## Cleaning and Maintenance

Cleaning: Clean the mixer and other reusables (between 2-3 operators it will take about 3-4 hour to complete). Fill the main mixer with water until dispersion blade is submerged and stir for 0.5-2 hours with moderate heating (30-40°C? let the vapor clean the mixer ceiling). Remove the dispenser valve for cleaning. Water wipe then acetone to dry.

Maintenance: Yearly maintenance is recommended to change dispersion rotor bearing and motor belt.

# Anode PressSlit

Process settings and quality targets for the anode pressing (calendering) and slitting steps.

## Pre-set Conditions

| Room Dew Point (°C) | <-20 |
| --- | --- |
| Room Temperature (°C) | 23 |

## Pressing Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Roll Linear Pressure (ton/cm) |  | 4.5 |  |
| O/S Roll Static Pressure (bar) |  | 100 |  |
| D/S Roll Static Pressure (bar) |  | 100 |  |
| O/S Roll Back Pressure (bar) |  | 100 |  |
| D/S Roll Back Pressure (bar) |  | 100 |  |
| Press Speed (m/min) |  | 12.0 |  |
| Press Roll Position 1 - O/S (mm) |  | 84.075 |  |
| Press Roll Position 1 - D/S (mm) |  | 83.890 |  |
| Press Roll Position 2 - O/S (mm) |  | 84.240 |  |
| Press Roll Position 2 - D/S (mm) |  | 84.060 |  |
| U/W Tension |  | 120 |  |
| R/W Tension |  | 140 |  |

## Pressing Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Press Thickness First Press (µm) |  | 159 ±3 |  |
| Press Thickness Final (µm) |  | 138 ±3 |  |
| Pres Thickness Springback (µm) |  | 142 ±3 |  |
| Loading Level (mg/cm2) |  | 21.9 ±0.3 |  |
| Press Density (g/cm3) |  | 1.54 -0.03 |  |
| Moisture Content (ppm) |  | <350 |  |
| Tensile Strength Test (N) |  | ≥1.3 |  |

## Slitting Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Slitting Speed (m/min) |  | 20 |  |
| U/W Tension (N) |  | 80 |  |
| R/W Upper Tension (N) |  | 90 |  |
| R/W Lower Tension (N) |  | 90 |  |
| Knife Incidence Angle (mm) |  | 0005 |  |
| Knife Exit Angle - Upper (mm) |  | 9905 |  |
| Knife Exit Angle - Lower (mm) |  | 0090 |  |
| Knife Speed - Upper (%) |  | 105 |  |
| Knife Speed - Lower (%) |  | 102 |  |
| Knife Overlap (mm) |  | 0.15 |  |
| Knife Unit Spacer Height (mm) |  | 9.85 |  |

## Slitting Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
|  |  | Left (Upper) | Right (Lower) |
| Coat Width (mm) |  | 121.4 ±0.25 | 121.4 ±0.25 |
| Uncoated Width (mm) |  | 15.6 ±0.25 | 15.6 ±0.25 |
| Coat Thickness (µm) |  | 142 ±3 | 142 ±3 |
| Curvature over 3m (mm) |  | <15 | <15 |
| Curl Height (mm) |  | <4 | <4 |
| # Pinholes |  |  |  |
| # Other Defects |  |  |  |

## Notes

Same slitter as cathode.

Highlighted cells are variable parameters, adjusted every batch or as needed.

## Note on Anode Press/Slit maintenance

Every 300-500 meters, wipe the main roll and nip rolls with water then acetone on cleanroom wipes (anti-dust/static).

Anode main roll is equipped with a cleaning mechanism (scraper); however, this doesn't work very well and requires manual cleaning.

Guide roll (press + slit) needs cleaning about once a week.

Change the rolls as needed (defect or damage) and equip with spares.

Knife maintenance: replace when there is a chip or breakage.

# Cathode Mix

## Pre-set Conditions

| Room Dew Point (°C) | <-20 |
| --- | --- |
| Room Temperature (°C) | 23 |
| Chiller Temperature (°C) | 7 |

## Raw Materials

| Category | Product |  | Phase | Input mass (kg) | Dry mass (kg) | Solid comp (%) | Supplier note |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CAM | NMC-622 |  | powder | 75.000 | 75.000 | 97.5% | Umicore |
| Binder 1 | PVDF Solef 5130 |  | solid | 0.231 | 0.231 | 1.0% | Solvay |
| Binder 2 | PVDF Solef 6020 |  | soild | 0.538 | 0.538 |  |  |
| Additive | Super-P |  | solid | 1.154 | 1.154 | 1.5% | Imerys/C-nergy |
| Solvent | NMP |  | liquid | 18.000 | N/A | N/A | Jaewon |

Batch totals: solid content 81.0%, total mass 94.923 kg, total volume 34.5 L.

## KPI Output

| Measurement |  | Target value | Range |
| --- | --- | --- | --- |
| Slurry Viscosity (cP) S65, 5 rpm |  |  |  |
| Slurry Viscosity (cP) S65, 50 rpm |  | 5,200 | ±200 |
| Slurry Particle Size (µm) |  | <20 | store image |
| Slurry Density at 23°C (g/cm3) |  | 2.75 |  |
| Slurry Solid Content (wt%) |  | 81.0 | ±1 |

## Additional Notes on Cathode Mixing

Viscosity is the primary metric to achieve within target value.

When adding powder, ramp up agitation speed from the lowest setting (5/100 rpm) and increase in 2 to 5 or 100 rpm increments until all loose powder is incorporated. Start with Dispersion blade. Scrape the agitation blades after every powder addition step (i.e. NMC, Super-P).

Pay close attention to the slurry temperature - very important for meeting the viscosity target consistently.

Make sure the chiller is always connected to the main tank and running.

Viscosity can increase after degassing step.

For other troubleshooting, refer to the "OCAP" tab.

## Cathode Recipe Steps

| Equipment | Step | Process |  | Amount (kg) | Solid Content (%) | RPM |  | Time (min) | Target Slurry Temp (°C) | Target Viscosity (cP) | Vessel Pressure | Note |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Planetary | Dispersion |  |  |  |  |  |
| Pre-Mixer | 1 | Add NMP |  | 8.846 | 8.0% | N/A | 400 | 4-6 hours or until dissolved | 20-23 | 2400 ±200 | atm |  |
|  | 2 | Add PVDF Solef 5130 |  | 0.231 |  |  |  |  |  |  |  |  |
|  | 3 | Add PVDF Solef 6020 |  | 0.538 |  |  |  |  |  |  |  |  |
| <Transfer> | 4 | Transfer to Main Mixer and measure viscocity |  |  |  |  |  |  |  |  |  |  |
| Main Mixer (100L) | 5 | Add Super-P |  | 1.154 | 17.9% | 20 | 1500 | 90 |  |  | atm | scrape blade |
|  | 6 | Add NMC-622 |  | 25.000 | 75.3% | 10 | 300 | 5 |  |  | atm | scrape blade |
|  | 7 | Add NMC-622 |  | 25.000 | 85.4% | 10 | 300 | 5 |  |  | atm | scrape blade |
|  | 8 | Add NMC-622 |  | 25.000 | 89.7% | 10 | 300 | 5 |  |  | atm | scrape blade |
|  | 9 | Add NMP |  | 4.000 | 85.7% | 10 | 300 | 30 |  |  | atm | Expect temp rise to ~40°C (Temp rise to <48°C for 150L) |
|  | 10 | Scrape blades and continue mixing |  |  |  | 20 | 1500 | 90 |  |  | atm |  |
|  | 11 | Add NMP |  | 2.000 | 83.8% | 20 | 1500 | 30 |  | >15,000 | atm | Set chiller temp to 10°C |
|  | 12 | Add NMP |  | 2.500 | 81.6% | 20 | 1500 | 30 |  | 5,500-6,500 | atm |  |
|  | 13 | Add NMP (adjustment) |  | 0.600 | 81.1% | 20 | 1500 | 30 |  | 4,500-5,200 | atm | Measure solid content, Hegman |
|  | 14 | Degas the slurry mixture (-0.08 MPa) |  |  |  | 5 | 0 | 30-60 |  |  | -0.08 MPa |  |
|  | 15 | Stabilize the slurry |  |  |  | 5 | 0 | 30-60 |  |  | atm |  |
|  | 16 | Measure viscosity and density (before transferring to coating) |  |  |  |  |  |  |  | 5,200 ±200 |  | Measure density |

## Cleaning and Maintenance

Cleaning: Clean the mixer, pre-mixer, and other reusables (between 2-3 operators it will take about 3-4 hour to complete). Water wipe to solidify the slurry residue and scrape off the solids. Remove the dispenser valve for cleaning. Finish off with acetone to dry.

Maintenance: Yearly maintenance is recommended to change dispersion rotor bearing and motor belt.

# Cathode CoatDry

Pre-set room and equipment conditions for cathode coating and drying, followed by the A-side and B-side coating, drying, and results parameters.

## Pre-set Conditions

| Room Dew Point (°C) | <-45 |
| --- | --- |
| Room Temperature (°C) | 23 |
| Foil Type | Al |
| Al Foil Thickness (µm) | 12 |
| Shim Width (mm) | 232.5 |
| Shim Internal Angle (°) | 84.5 |
| Shim Rounding | C 3/4 |
| Shim Thickness (T) | 1.2 |

## Slurry Supply Unit

| Slurry Temperature (°C) | 23 |
| --- | --- |
| Slurry Mixer Motor Speed (rpm) | 20 |
| Overnight Slurry Circulation | NO |
| Slurry Pump Servo Circulation (rpm) | 20-30 |
| Slurry Pump Servo Side A (rpm) | 35-37 |
| Slurry Pump Servo Side B (rpm) | 35-37 |
| Magnetic Filter | YES |
| Mesh Filter (µm) | 125 (<115 µm) |

## Cathode Coater Maintenance

Wipe the rollers when there is a change in slurry chemistry/composition.

Use acetone and cleanroom wipes (anti-dust/static) to wipe the rollers.

Change the rolls as needed (defect or damage) and equip with spares.

## A Side

## Coating Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Total Foil Width (mm) |  | 270.0 |  |
| Coat Width (mm) |  | 234.0 |  |
| Uncoated Width (mm) |  | 18.0 |  |
| Slot Die Dispense Pressure (MPa) |  | 0.007-0.008 |  |
| Slot Die Gap D/S (µm) |  | 136.0 |  |
| Slot Die Gap O/S (µm) |  | 136.0 |  |
| Slot Die Tilt (°) |  | 0 |  |
| Nip Roll Pressure D/S |  | 6 |  |
| Nip Roll Pressure O/S |  | 6 |  |
| Line Speed (m/min) |  | 6 |  |
| U/W Tension (N) |  | 80 |  |
| Outfeed Tension (N) |  | 90 |  |
| Rewind Tension (N) |  | 90 |  |

## Drying Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Zone 1 Temperature (°C) |  | 131 |  |
| Zone 2 Temperature (°C) |  | 125 |  |
| Zone 3 Temperature (°C) |  | 118 |  |
| Zone 4 Temperature (°C) |  | 118 |  |
| Zone 1 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 2 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 3 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 4 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 1 Circulation Opening (%) |  | 30 |  |
| Zone 2 Circulation Opening (%) |  | 30 |  |
| Zone 3 Circulation Opening (%) |  | 30 |  |
| Zone 4 Circulation Opening (%) |  | 30 |  |

## Coating Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Loading Level A Side (mg/cm2) |  | 21.0 ± 0.3 |  |
| Coat Thickness after Drying (µm) |  | 88-92 |  |
| Coat Width (µm) |  | 234.0 ±0.5 |  |
| Uncoated Width (µm) |  | 18.0 ±0.25 |  |

## B Side

## Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Total Foil Width (mm) |  | 270.0 |  |
| Coat Width (mm) |  | 234.0 |  |
| Uncoated Width (mm) |  | 18.0 |  |
| Slot Die Dispense Pressure (mPa) |  | 0.007-0.008 |  |
| Slot Die Gap D/S (µm) |  | 208.0 |  |
| Slot Die Gap O/S (µm) |  | 202.0 |  |
| Slot Die Tilt (°) |  | 0 |  |
| Nip Roll Pressure D/S |  | 6 |  |
| Nip Roll Pressure O/S |  | 6 |  |
| Line Speed (m/min) |  | 6 |  |
| U/W Tension (N) |  | 80 |  |
| Outfeed Tension (N) |  | 90 |  |
| Rewind Tension (N) |  | 90 |  |

## Drying Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Zone 1 Temperature (°C) |  | 131 |  |
| Zone 2 Temperature (°C) |  | 125 |  |
| Zone 3 Temperature (°C) |  | 118 |  |
| Zone 4 Temperature (°C) |  | 118 |  |
| Zone 1 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 2 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 3 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 4 Circulation Fan Speed (rpm) |  | 3300 |  |
| Zone 1 Circulation Opening (%) |  | 30 |  |
| Zone 2 Circulation Opening (%) |  | 30 |  |
| Zone 3 Circulation Opening (%) |  | 30 |  |
| Zone 4 Circulation Opening (%) |  | 30 |  |

## Coating Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Loading Level AB Side (mg/cm2) |  | 42.0 ± 0.3 |  |
| Coat Thickness after Drying (µm) |  | 176-184 |  |
| Coat Width (µm) |  | 234.0 ±0.5 |  |
| Uncoated Width (µm) |  | 18.0 ±0.25 |  |
| AB Mismatch (mm) |  | <0.2 |  |
| High Edges? |  | NO |  |
| Crack Test |  | PASS |  |
| Peel Test |  | PASS |  |

# Cathode PressSlit

## Pre-set Conditions

| Room Dew Point (°C) | <-45 |
| --- | --- |
| Room Temperature (°C) | 23 |

## Pressing Process Conditions

Highlighted parameters are variable: some are set every batch, others adjusted as needed.

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Roll Linear Pressure (ton/cm) |  | 4.9 |  |
| D/S Roll Static Pressure (bar) |  | 110 |  |
| O/S Roll Static Pressure (bar) |  | 110 |  |
| D/S Roll Back Pressure (bar) |  | 100 |  |
| O/S Roll Back Pressure (bar) |  | 100 |  |
| Press Speed (m/min) |  | 12.0 |  |
| Press Roll Position - D/S (mm) |  | 84.880 |  |
| Press Roll Position - O/S (mm) |  | 84.665 |  |
| U/W Tension |  | 120 |  |
| Infeed Tension |  | 50 |  |
| Outfeed Tension |  | 50 |  |
| R/W Tension |  | 140 |  |
| IHA Power (kW) |  | 1.6 |  |
| Pre-Heat Temp (°C) |  | OFF |  |
| Press Roll Target Temp (°C) |  | OFF |  |

## Pressing Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Coat Thickness (µm) |  | 117.5 ±3 |  |
| Loading Level (mg/cm2) |  | 41.3 ±0.3 |  |
| Press Volume Density (g/cm3) |  | 3.51 ±0.10 |  |
| Moisture Content (ppm) |  | <250 |  |
| Crack Test |  | PASS |  |
| Peel Test |  | PASS |  |

## Slitting Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Slitting Speed (m/min) |  | 20 |  |
| U/W Tension (N) |  | 80 |  |
| R/W Upper Tension (N) |  | 120 |  |
| R/W Lower Tension (N) |  | 120 |  |
| Knife Incidence Angle (mm) |  | 9975 |  |
| Knife Exit Angle - Upper (mm) |  | 9930 |  |
| Knife Exit Angle - Lower (mm) |  | 0030 |  |
| Knife Speed - Upper (%) |  | 105 |  |
| Knife Speed - Lower (%) |  | 102 |  |
| Knife Overlap (mm) |  | 0.15 |  |
| Knife Unit Spacer Height (mm) |  | 9.85 |  |

## Slitting Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
|  |  | Left (Upper) | Right (Lower) |
| Coat Width (mm) |  | 117.0 ±0.25 | 117.0 ±0.25 |
| Uncoated Width (mm) |  | 18.0 ±0.25 | 18.0 ±0.25 |
| Coat Thickness (µm) |  | 117.5 ±3 | 117.5 ±3 |
| Curvature (mm) |  | <15 | <15 |
| Curl Height (mm) |  | <4 | <4 |
| Crack Test |  | PASS | PASS |
| # Pinholes |  |  |  |
| # Other Defects |  |  |  |

## Maintenance Notes

Wipe all rollers about once a week, or when there is a change in slurry chemistry/composition, with acetone on cleanroom wipes (anti-dust/static).

Main roll can be cleaned once a month.

Guide roll (press + slit) needs cleaning about once a week.

Change the rolls as needed (defect or damage) and equip with spares.

Knife maintenance: replace when there is a chip or breakage.

# Assembly

Room conditions, process parameters, and inspection results for the seven-stage cell assembly line.

## Pre-set Conditions

| Room Dew Point (°C) | <-45 |
| --- | --- |
| Room Temperature (°C) | 23 |

## Assembly Sequence

Winding and Vision System Check

JR Stacking

Pre Welding (Tab formation)

Insulation Taping

JR Insertion into Can

Main Welding

Can-Cap Welding, Hi-Pot Check, 3D Vision Check

## 1. Winding + Vision Process Condition

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| U/W Anode Tension (g) |  | 400 ± 100g |  |
| U/W Cathode Tension (g) |  | 400 ± 100g |  |
| U/W Separator Tension (g) |  | 300 ± 100g |  |
| Press Force 1 |  |  |  |
| Press Force 2 (T) |  | 1.0 |  |
| # of Turns |  | 19.3 |  |
| Main Winding Speed (mm/s) |  | 500 ± 30 mm/sec |  |
| Main Winding Acceleration (mm/s²) |  | 1000 mm/s² |  |
| Main Winding Deceleration (mm/s²) |  | 1000 mm/s² |  |
| Cathode/Anode Burr at cutting |  | < 15µm |  |
| Cathode length (mm) |  | 3200 |  |
| Anode length (mm) |  | 3390 |  |
| Sepa pre winding (Turn) |  | 1 |  |
| Anode pre winding (mm) |  | 188 |  |
| Main winding velocity (mm/s) |  | 500 |  |
| Remain winding (Turn) |  | 1.3 |  |
| Mandrel Perimeter (fixed, mm) |  | 100 |  |
| Mandrel width (fixed, mm) |  | 30 |  |
| Mandrel heightf (fixed, mm) |  | 60 |  |
| Sepa thickness (mm) |  | 13 |  |
| Cathode thickness (mm) |  | 130 |  |
| Anode thickness (mm) |  | 154 |  |
| Seal tape length |  | 122.5 |  |
| EPC Electrode Spool |  | (+3>X>-3) |  |
| EPC Separator Spool |  | (+3>X>-3) |  |
| EPC Electrode PIVOT |  | (+3>X>-3) |  |
| EPC Separator PIVOT |  | (+3>X>-3) |  |
| Final EPC |  | (+3>X>-3) |  |

## Vision Check Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| J/R Thickness (mm) |  | 12 |  |
| J/R Weight (g) |  | 315 ± 3g |  |
| Short Current (Mohm) |  | 2026-03-15 |  |
| Positive Distance[anode length] (mm) |  | 11.45 |  |
| Positive Sepa Distance[anode tape] (mm) |  | 2.55 |  |
| Negative Distance[cathode length] (mm) |  | 10.65 |  |
| Negative Sepa Distance[cathode tape] (mm) |  | 2.53 |  |
| JR Width (mm) |  | 152.7 ± 0.3 |  |
| Cathode Electrode Length (mm) |  | 3200 |  |
| Anode Electrode Length (mm) |  | 3390 |  |
| Cathode Separator Length (mm) |  | 3900 |  |
| Anode Separator Length (mm) |  | 3920 |  |
| Telescoping |  | Yes/No |  |
| Separator Wrinkle |  | Yes/No |  |

## 2. JR Stack Taping Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Taping Time (s) |  | 63 sec |  |
| Tape Width (mm) |  | 18 mm |  |
| Tape Length (mm) |  | 117 mm |  |

## Taping Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Pass/Fail |  | 1/0 |  |

## 3. Pre-Welding (Tab Formation)

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Welding Time (s) |  | 0.4 ± 0.2 sec |  |
| Anode Weld Amplitude (%) |  | 10 ± 3% |  |
| Cathode Weld Amplitude (%) |  | 40 ± 5% |  |
| J/R Press Pressure (kPa) |  | 400 |  |
| Weld Energy (J) |  | 350 ± 35 J |  |

## Pre-Welding Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| JR Trimmed Width (mm) |  | 32~55 |  |
| Weld Position Accuracy |  | 0.05 |  |
| X-ray Parameters |  |  |  |

## 4. Insulation Taping Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Recipe Time (s) |  | 65 ± 5 sec |  |
| Tape Width (mm) |  | 174 ± 1mm |  |
| Tape Length (mm) |  | 200 ± 1mm |  |

## Insulation Taping Results

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Pass/Fail |  | 1/0 |  |

## 5. Main Welding (Terminal to Cap Welding)

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Anode Welding Time (s) |  | 0.2 ± 0.1 sec |  |
| Cathode Welding Time (s) |  | 0.3 ± 0.1 sec |  |
| Anode Welding Pressure (MPa) |  | 0.2 ± 0.1 MPa |  |
| Cathode Welding Pressure (MPa) |  | 0.2 ± 0.1 MPa |  |
| Weld Energy (J) |  | 350 ± 35 J |  |

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Anode Ultrasonic Weld (%) |  | 14.9 |  |
| Cathode Ultrasonic Weld (%) |  | 24.5 |  |
| Anode Welding True Width (mm) |  | 3.7 x 11 (2 points) |  |
| Cathode Welding True Width (mm) |  | 3.7 x 11 (2 points) |  |
| Tensile strength |  | P/F |  |

## JR Insertion into Can Process Conditions

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Insertion Force (kgf) |  | 40 ± 10 kgf |  |

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Pass/Fail |  | 1/0 |  |

## Can-Cap Welding

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Hi Pot Recipe Check Time (s) |  | 53s |  |
| Hi-Pot Test Voltage (V) |  | DC 500V MAX |  |
| Vacuum Leak Recipe Time (s) |  | 15s ± 5 |  |
| Vacuum Check Pressure (Torr) |  | 70 |  |
| Laser gun focus distance |  | 0.45 ± 0.2mm |  |
| Welding speed |  | 60 ± 10mm/sec |  |
| Shield gas N2 amount |  | 30 ± 10 L/min |  |
| Protection glass condition |  | No defect - refer to top standard |  |
| Oscillator output |  | 1000 ± 200W |  |
| Pusher pressure - fixed |  | 0.4 ± 0.1 MPa |  |
| Pusher pressure - side |  | 0.15 +0.1/−0.5 MPa |  |
| Weld bead width |  | Min 1000µm |  |
| Weld bead depth |  | Min 800µm |  |
| Cell height (terminal to can bottom) |  | 101.3 ± 0.4 mm |  |
| Judgment current |  | Max 5 mA |  |

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Laser 3D Bead Parameters |  |  |  |
| Hi Pot Current (mA) |  | 0.129 |  |
| Vacuum Leak Min-Max Value |  | min 0 Torr. max 75 Torr |  |
| X-Ray Clearance 1 |  |  |  |
| X-Ray Clearance 2 |  |  |  |
| X-Ray Clearance 3 |  |  |  |
| X-Ray Clearance 4 |  |  |  |
| X-Ray Clearance 5 |  |  |  |
| X-Ray Clearance 6 |  |  |  |

## Seal Pin Welding

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| PFA Ball: Cell vacuum + ball insert |  | −80 ± 5 kPa / 60 hr |  |
| PFA ball: press force |  | 0.3 ± 0.15 MPa (no protrusion) |  |
| Laser gun focus distance |  | 6.17 ± 0.1mm |  |
| Welding speed |  | 560 ± 50 mm/sec |  |
| Shield gas N2 amount |  | 30 ± 10 L/min |  |
| Oscillator output |  | 3800 ± 500W |  |

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Laser 3D Bead Parameters |  |  |  |
| Hi Pot Current (mA) |  | 0.129 |  |
| Vacuum Leak Min-Max Value |  | min 0 Torr. max 750 Torr |  |
| X-Ray Clearance 1 |  |  |  |
| X-Ray Clearance 2 |  |  |  |
| X-Ray Clearance 3 |  |  |  |
| X-Ray Clearance 4 |  |  |  |
| X-Ray Clearance 5 |  |  |  |
| X-Ray Clearance 6 |  |  |  |

# Finishing

Cell finishing covers electrolyte fill, high-temperature wetting, pre-charging, and final sealing.

## Pre-set Conditions

| Room Dew Point (°C) | <-45 |
| --- | --- |
| Room Temperature (°C) | 23 |

## 1st Electrolyte Fill - Process Conditions

| Fill Quantity (g) | 140 |
| --- | --- |
| Vacuum (Torr) | 0.02 |
| Pressure (Torr) | 75 |
| # Vacuum Cycles | 2 |
| # Pressure Cycles | 1 |

## 1st Electrolyte Fill - Results

| Mass Before Fill (g) | 770 |
| --- | --- |
| Mass After Fill (g) | 910 |

## HT Wetting - Process Conditions

| Process Time (h) | 24 |
| --- | --- |
| Temperature (°C) | 45 |

## Pre-Charging - Process Conditions

| Pre-Charge Time (min) | 120 |
| --- | --- |
| Pressure (bar) | 3.6 |
| Pre-Charge Current (mA) | 5000 (0.1 C) |
| Pre-Charge SOC (%) | 20 |

## Pre-Charging - Results

| Cell Voltage (V) | 3.5 |
| --- | --- |

# Formation

## Room Conditions

| Room Dew Point (°C) | ambient |
| --- | --- |
| Room Temperature (°C) | 23 |

## IR/OCV Check and Formation

The formation and quality-control sequence steps through IR/OCV checks, formation charge/discharge cycles, and a 15-day aging period.

| # | Sequence |  | Step |  | Time (min) | Current (A) | Voltage Limit (V) | Cut-Off Current (mA) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | IR/OCV Check #2 |  | IR2 (mohm) | <0.8 | 5 |  |  |  |
|  |  |  | OCV2 (mV) | 3430 ± 15 |  |  |  |  |
| 2 | 1st Formation |  | Charge CC at 1C, CV to 0.05C |  | 60 | 48.5 | 4.2 | 2.5 |
| 3 |  |  | Rest |  | 10 |  |  |  |
| 4 |  |  | Dsch to 3.0 V, 1C |  | 60 | 48.5 | 3.0 |  |
| 5 |  |  | Rest |  | 10 |  |  |  |
| 6 |  |  | Charge CC at 1C |  | 30 | 48.5 | 3.665 |  |
| 7 | IR/OCV Check #3 |  | IR3 (mohm) | <0.8 |  |  |  |  |
|  |  |  | OCV3 (mV) | 3665 ± 15 |  |  |  |  |
| 8 | 15-Day Aging at r.t. |  |  |  | 15 days |  |  |  |
| 9 | IR/OCV Check #4 |  | IR4 (mohm) | <0.8 |  |  |  |  |
|  |  |  | OCV4 (mV) | 3655 ± 15 |  |  |  |  |
|  |  |  | ΔOCV | <0.5% | ΔOCV = {(OCV4 - OCV3)/OCV3} |  |  |  |
| 10 | 2nd Formation |  | Charge to 4.2 V, 1C |  | 60 | 50 | 4.2 | 2.5 |
| 11 |  |  | Rest |  | 10 |  |  |  |
| 12 |  |  | Discharge to 3.0 V, C/2 |  | 120 | 25 | 3.0 |  |
| 13 |  |  | Rest |  | 10 |  |  |  |
| 14 |  |  | Charge to 3.6V, 1C |  | 20 | 50 | 3.6 |  |
| 15 | IR/OCV Check #5 |  | IR5 (mohm) | <0.8 |  |  |  |  |
|  |  |  | OCV5 (mV) | 3600 ± 15 |  |  |  |  |

## Dimension + Weight Check (Post-Formation)

| Parameter |  | Value |  |
| --- | --- | --- | --- |
| Height 1 (mm) |  | 94.8 ± 0.5 |  |
| Height 2 (mm) |  | 101.3 ± 0.7 |  |
| Height 3 (mm) |  | 94.8 ± 0.5 |  |
| Height 4 (mm) |  | 101.3 ± 0.7 |  |
| Height 5 (mm) |  | 94.8 ± 0.5 |  |
| Thickness 1 (mm) |  | 29-30.6 (29.2:-0.2+1.4) |  |
| Thickness 2 (mm) |  |  |  |
| Thickness 3 (mm) |  |  |  |
| Thickness 4 (mm) |  |  |  |
| Thickness 5 (mm) |  |  |  |
| Weight (g) |  | 900 ± 10 |  |

## Ready-to-Ship Criteria

ΔOCV is <0.5%.

2nd Formation Discharge (Step 3) Capacity is 48.5 Ah +/- 1.

IR5 is <0.8 mOhm.

Dimension and weight checks pass.

# ElectrodeAssembly OCAP

This out-of-control action plan (OCAP) lists process issues that can be observed across electrode assembly, their spec limits, the corrective action to take, and a likelihood and severity rating for each.

## Rating Scales

The Likelihood and Severity columns in the table below use these three-point scales.

| 1 | Rare occurrence |
| --- | --- |
| 2 | Some occurrence |
| 3 | Possibly encountering every batch |

| 1 | Minimal material loss |
| --- | --- |
| 2 | Some material loss |
| 3 | May require batch restart |

## Out-of-Control Action Plan

| Process (where the issue was observed) | Description of "Out-of-Control" Issue | spec | Action Plan | Likelihood of Occurence (for stable process) | Severity of Issue | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Mixing | Slurry viscosity is lower than spec. Anode < 6,500 - 500 Cathode < 5,250 - 500 |  | Discard if not possible to proceed with coating. Initiate RCA by checking mixing temp profile and active lot ID, IQC results, and storage condition. | 2 | 2 | Addressable at coating within limits. |
| Mixing | Slurry viscosity is higher than spec. Anode < 6,500 + 500 Cathode < 5,250 + 500 |  | Add more solvent. Use the solvent addition calculator as a guide. | 2 | 1 |  |
| Mixing | Larger than spec agglomerates are observed. Anode <30 µm Cathode <20 µm |  | Filter out agglomerates in slurry supply unit at the coater. Discard if not possible to proceed with coating. Initiate RCA by checking mixing agitation and temp profile and active lot ID, IQC results, and storage condition. | 1 | 3 |  |
| Mixing | Slurry is not stabilized or fully homogeneous. |  | Discard if not possible to proceed with coating. Initiate RCA by checking mixing agitation and temp profile and active and binder lot ID, IQC results, and storage condition. | 1 | 3 |  |
| Mixing | Solid content is lower than spec. Anode 50 ±3 Cathode 80 ±3 |  | Add more solids. Adjust carefully as this will impact viscosity and is important for coating. Add in small increments of the target (e.g. 25-50% at first), control the shear to allow wet-out time, recheck viscosity, and only add solids and solvent as necessary. | 1 | 1 | Impacts drying |
| Mixing |  |  |  |  |  |  |
| Coating/Drying | Pump speed needs to be increased for slurry (stability, bubbles, viscosity issues, etc). |  | Increase the pump speed and the slot die gap simultaneously. Expect that increasing the pump speed will increase the coating width - so the die gap needs to be adjusted. Loading will increase so discretional increase is recommended. | 1 | 2 |  |
| Coating/Drying | Loading level profile - center-high |  |  | 2 | 2 |  |
| Coating/Drying | Loading level profile - edge-high |  | Decrease the slot die gap. This will increase the coating width slightly but +/- 0.5 mm coating allowance is accounted for. If low viscosity is the issue, adjust the shim width (the relationship between shim width and viscosity spec needs to be established for double lane). | 2 | 2 | Can happen when viscosity is low. Serious issue that will propagate quickly through the rest of electrode processing and detrimental to winding. At SH, when viscosity is lower by 1000 cP, they reduce the shim width by 6 mm (for which slurry needs further clarification). |
| Coating/Drying | Loading level profile - wavy |  | Adjust the slot die gap. May become resolved as coating stabilizes. | 2 | 2 | Good mixing is important. Lower solids (low 70) is desirable but we are using ~80 wt%. |
| Coating/Drying | Uncoated edge is turning upward |  | Drying temp setting may be too high. Lower the temp. | 1 | 2 |  |
| Coating/Drying | Binder migration ("splotchy" appearance of the dried electrode, i.e. irregular spots or patches) |  |  | 1 | 2 |  |
| Coating/Drying | Cracks are observed in the coat |  |  | 1 | 2 |  |
| Coating/Drying | Poor cohesion or out-out-spec KF results (too high) for dried anode electrode |  | Adjust the temp profile - use stepwise decrease, increase temp in zone 1 & 2. | 1 | 2 |  |
| Coating/Drying |  |  |  |  |  |  |
| Pressing | Wrinkles in the uncoated area |  | This means that tension balance is off - adjust to lower tension. | 1 | 1 |  |
| Pressing | Anode - coat/uncoated interface is wavy |  | Main roll pressure is too high - lower press linear pressure. | 1 | 2 |  |
| Pressing | Anode - defect observed in the coat |  | Stop the line and check for regularity of defect along the coating direction as well as debris on main roll. Clean the main roll before resuming. | 2 | 2 |  |
| Pressing |  |  |  |  |  |  |
| Pressing |  |  |  |  |  |  |
| Pressing |  |  |  |  |  |  |
| Slitting | Severe curvature out of spec limits |  | Adjust press and/or slit U/W and R/W tension, line speed. For cathode, increasing IHA power can be considered (less desired due to downstream effects in welding) as well as position of the IHA source. | 1 | 3 | SH team recommends purchasing a rewinder for post-slitting step. |
| Slitting |  |  |  |  |  |  |
| Slitting |  |  |  |  |  |  |
| Winding | Non-compliance with jelly roll weight standards |  | docs.google.com/…/edit | 1 | 2 |  |
| Winding | Failure to meet insulation resistance / misalignment short |  | docs.google.com/…/edit | 1 | 3 |  |
| Winding | Jelly roll damage / Inclusion of foreign substances |  | docs.google.com/…/edit | 1 | 3 |  |
| Winding | Jelly roll telescoping |  | docs.google.com/…/edit | 2 | 3 |  |
| Pre-Welding | Tab damage / welding defect / insufficient weld strength |  | docs.google.com/…/edit | 2 | 3 |  |
| Main Welding | Tab damage / welding defect / insufficient weld strength |  | docs.google.com/…/edit | 2 | 3 |  |
| Can Cap laser welding | CanCap damage / welding NG / weld depth NG |  | docs.google.com/…/edit | 2 | 3 |  |
| Taping and insertion | Jelly roll damage / taping defect (bare electrode area exposed) |  | docs.google.com/…/edit | 2 | 3 |  |
| Efilling | Electrolyte backflow / insufficient fill / cross-contamination with different electrolyte |  | docs.google.com/…/edit | 2 | 3 |  |